# Biofunctionalized carbon nanotubes as a smart nanomaterial immobilized on tissue culture polystyrene plates for promoting neuronal outgrowth

Source: Research Square preprint, posted 2022-09-30. DOI: 10.21203/rs.3.rs-2108449.

URL: https://www.researchsquare.com/article/rs-2108449/v1

Authors: Hyun-Soo Kim, Kam W. Leong, Gi Jin Kim, Ueon Sang Shin, Hae-Won Kim, Ji-Young Hwang.

Licensed under a Creative Commons Attribution (CC BY 4.0) license. This preprint has not been peer reviewed by a journal. This excerpt (abstract and introduction) is reproduced verbatim as raw material for a before/after editing sample.

Abstract

Carbon nanotubes (CNTs) exhibit attractive attributes that make them useful as an innovative biomaterial for neuroscience research. These include their nanoscale features, modifiable chemical functionality, and tunable electrical properties. In this study, we developed a simple and cost-effective method for fabricating surface-modified cell culture systems by immobilizing biofunctionalized CNTs onto commercial tissue culture polystyrene plates. This active substrate was then examined to understand how electrical, morphological, and chemical interactions with a CNT-entrapped phosphatase and tensin homolog deleted on chromosome 10 (PTEN) inhibitor, namely, bisperoxovanadium (bpV), affect the neuronal differentiation of PC-12 cells. Compared with the control, the percentage of neuronal cells bearing neurites increased by a factor of 4.0, 7.8, and 10.0 when cultured, respectively, on an immobilized carboxylated CNT substrate, a poly(ethylene glycol) (PEG)ylated CNT substrate, and a bpV-loaded PEGylated CNT substrate (10 nM bpV). The bpV-loaded CNT substrate down-regulated the expression of PTEN and activated the Akt/ERK signaling pathway, thereby providing a mechanism for the improved neuronal outgrowth. These results highlight the promise of biofunctionalized CNTs as an electroactive and drug-releasing smart nanomaterial for promoting neuronal outgrowth and suggest that they may be useful in future neural regeneration applications.

Keywords: carbon nanotubes, biofunctionalization, surface-modified tissue culture plate, drug delivery system, PTEN inhibitor, neuronal outgrowth, neural regeneration

## 1. Introduction

Parallel advances in nanotechnology and tissue engineering over the past decades have spurred the design and development of smart biomaterials through multidisciplinary approaches. Numerous convergence studies have been attempted to regenerate neural tissue, one of the most difficult tasks in tissue engineering and regenerative medicine.

Bioinspired nanocomposites for nerve tissue repair and neural regeneration require substrates that exhibit several key properties. These include topographical surfaces, improved attachment to neuronal cells for proliferation and/or differentiation, and the capacity for the sustained release of biofunctional factors. These materials should also exhibit mechanical integrity, controllable biodegradability, and good biocompatibility with the nanoscale reinforcements that are being employed in a broad range of applications [1–8].

Among the various nanomaterials being explored, carbon nanotubes (CNTs), which possess unique electrical, mechanical, physical, and chemical properties, are a popular choice for smart biomaterials. CNTs are already being used in various basic and applied neuroscience research applications [9–14]; however, concerns remain regarding the cytotoxicity and genotoxicity of CNTs with respect to both in vitro and in vivo applications [15–19]. The toxicity of CNTs may be countered by modifying them with biocompatible moieties and by immobilizing the CNTs onto the surfaces of other materials suitable for biomedical applications [20].

Thus, the biofunctionalization of CNTs can address their toxicity while also expanding their functionality by promoting cell attachment, neuronal outgrowth, neuronal differentiation, and nerve tissue regeneration [21]. Interactions between neural cells and CNT substrates, which are used as an alternative to directly adding CNTs to the neuronal culture medium, have been explored to reduce the toxicity of CNTs and improve their utility in implantable devices and cell-guiding scaffolds [14, 22].

Significant efforts have been made to develop drug delivery systems that allow drugs to be delivered to the target tissue or cells. Efficient drug capture systems based on CNT substrates require polyethylene glycol (PEG) coatings, that is, PEGylation, to allow for the incorporation of both water-insoluble and water-soluble drugs for controlled release into an aqueous medium via nanoscale extraction to improve neural regeneration [23–25]. The PEGylation of CNTs, which are hydrophobic, improves their dispersibility and increases their hydrodynamic size, and decreases their immunogenicity, thereby reducing their cytotoxicity [18, 26]. This work describes an efficient system for loading and releasing the drug bisperoxovanadium (bpV), which acts as a potent inhibitor of the protein tyrosine phosphatase (PTPase) activity of phosphatase and tensin homolog deleted on chromosome 10 (PTEN) as well as an enhancer of neurite outgrowth [27–29].

This study explores the use of biofunctionalized CNT substrates in enhancing neuronal cell outgrowth. Four types of CNT substrates were evaluated: i) a commercial culture plate (CP) and pristine CNTs, ii) a CP with functionalized CNTs subjected to carboxylation and covalent crosslinking onto the CP surface (CP-CNT-COOH), iii) CNTs subjected to PEGylation (CP-CNT-PEG-NH2), and iv) CNTs biofunctionalized on a PEGylated CNT substrate (CP-CNT-PEG + drug) for a smart drug delivery system (DDS). Various analyses of the neuronal outgrowth were then performed to assess the potential of these biofunctionalized CNT substrates for nerve tissue regeneration and biomedical applications (Fig. 1). For each substrate, we assessed cell viability and analyzed neuronal outgrowth, drug-stimulated differentiation, and the underlying pathways activated in the cultured cells. Neuronal outgrowth was promoted by the electrical conductivity of the CNT substrates and the controlled release of the drug.