# Physics-assisted machine learning methods for cracking performance of recycled aggregate concrete

Source: Research Square preprint, posted 2022-10-24. DOI: 10.21203/rs.3.rs-2173524.

URL: https://www.researchsquare.com/article/rs-2173524/v1

Authors: Xiangyu Han, Kai Cui, Qinghua Xiao.

Licensed under a Creative Commons Attribution (CC BY 4.0) license (https://creativecommons.org/licenses/by/4.0/). This preprint has not been peer reviewed by a journal. This excerpt (abstract and introduction) is reproduced verbatim as raw material for a before/after editing sample.

## Abstract

The poor cracking performance of recycled aggregate concrete (RAC) has become an obstacle to its application; however, predicting its performance is difficult. In this study, physics-assisted machine learning methods are adopted to predict the cracking performance of RAC. Based on physics, nine features are selected as the input variables, while the splitting tensile strength is selected to characterize cracking. The classification and regression trees, support vector regressor, adaptive boosting (Adaboost), and random forest algorithms are used to construct the predictive models, and the firefly algorithm is used to search for the optimum hyperparameters. On comparing the predicted values with the experimental data during the training and testing procedures, the Adaboost model is found to be the best one for predicting the tensile strength of RAC. When combined with the physical mechanism, this analysis shows that the recycled aggregate content, aggregate size, and water content are the three most influential factors for predictive models, and that these factors should be carefully considered when designing the RAC mixture. Moreover, the reliability of the predictive models is verified by physical experiments.

## Introduction

Owing to its various outstanding characteristics, concrete is used widely in building construction. According to the National Development and Reform Commission of China, the total production of commercial concrete exceeded 32 billion cubic meters in 2021. Hence, large amounts of cement, sand, natural gravel, and crushed stone are required every year. Meanwhile, with the demolition of old and abandoned buildings, more than 2 billion tons of concrete waste is produced annually. As a result, recycled aggregate concrete (RAC), which uses recycled concrete waste to partly replace the coarse aggregates in concrete, is increasingly being used. This development is also helping reduce the carbon emissions related to concrete production.

During the production of the recycled aggregates, the final product typically consists of natural aggregates and hardened mortar. Hence, compared with natural aggregates, the recycled aggregates exhibit low strength owing to the presence of the hardened mortar, which is weaker, and the interfaces that form between the mortar and the aggregates. Furthermore, many cracks are generated within the recycled aggregates during the crushing process. As shown in Fig. 1, several weak regions are introduced into RAC, making it particularly prone to cracking under external loads and thus severely restricting its applicability. Consequently, compared with its other mechanical properties, the cracking characteristics of RAC deserve more attention.

Fiber-reinforced RAC, which is a type of RAC, exhibits greater cracking resistance because of the fibers present. Akca et al. used polypropylene fibers to reinforce RAC and showed that both the flexural tensile strength and splitting tensile strength increased with the fiber content. Ali et al. compared the mechanical properties of glass-fiber-reinforced RAC and plain RAC. They observed that the splitting tensile strength of the fiber-reinforced RAC was markedly higher. Gao et al. studied the performance of steel-fiber-reinforced RAC and found that the flexural strength improved significantly with an increase in the steel fiber volume fraction. Thus, it can be concluded that fibers are effective in improving the cracking resistance of RAC. However, their reinforcement performance is affected by various factors.

For plain concrete, various methods have been proposed to predict its cracking performance, such as fracture tests, numerical methods, and mechanical models. In addition, different factors have been evaluated to test the reliability of its performance prediction. However, precisely describing its cracking characteristics remains difficult. Given the effect of the recycled aggregates, predicting the cracking behavior of RAC, especially that of fiber-reinforced RAC, is even more complex. Machine learning (ML) methods are novel approaches for prediction problems. Pan and Amin used ML to predict the cracking characteristics of RAC and established several ML models with superior performance. However, during the construction of the ML models, the physical meaning of the models was neglected, and the effect of any reinforcing fibers was not considered.

In this study, the existing mechanical models and the results of physical experiments are adopted to improve the ML approaches with the aim of predicting the cracking behavior of RAC accurately. The rest of the paper is arranged as follows: Section 2 mainly describes the construction of a database based on physical theories; Section 3 illustrates the various ML algorithms used in this study; Section 4 mainly presents the construction process of predictive models; Section 5 describes the results of tests performed using the predictive models and compares them with those of mathematical and physical methods; and finally Section 6 lists the conclusions.